Selected properties of geopolymers with different portions of ground fly-ash

Abstract: Geopolymers are polymeric materials resulting from the polycondensation reaction of alumino-silicate materials in a strongly alkaline environment. In the consequence, stable polymeric networks of aluminosilicates are formed. The binding potential of FA (fly ash) amorphous component can also be “activated” by mechanical activation, which unfolds new possibilities of FA utilization. Mechanical activation, as a method which can improve FA reactivity, is often applied for different applications for geopolymers based on ground fly ash. This paper presents possibilities of preparing of geopolymer mixtures based on modified (ground) FA (TEKO – produced by the Heating plant Kosice), which was used in varying percentages to unground (original) FA. The particle size of original unground FA (PVT) was 84.7μm and particle size of ground FA (T60S1) was 52.8μm. Properties to be evaluate were selected from expected application point of view – protective coating of concrete. Next properties of geopolymer mixtures after 28 days of hardening were tested and evaluated: dry density, absorptivity, capillarity, compressive and flexural strength.

Keywords: geopolymer, fly ash - FA, strength, absorptivity, capillarity

- Introduction

Construction industry provides great and significant amount of options for use of industrial wastes in manufacturing of some building materials, or in the development of new ones. The global development of consumer society, however, leads to an enormous increase in waste production and problems with their disposal, therefore necessity of processing the wastes even at higher energy expense and final cost, is discussed still more (Rai  A. and Rao D.B.N., 2005).

Worldwide, millions of tons of fly ash are generated each year by coal-fired power plants satisfying the large demand for industrial and domestic energy. In Slovakia, a majority of fly ashes are hydraulically transported to settling basins or extracted mines and only a small amount of fly ashes is utilized. The deposited fly ashes are being exposed to exogenous and biogenous factors that change their chemical and structural composition and become harmful to the environment (Michalíková et al., 2003). Therefore, a large numbers of researchers have been aimed on the utilization of this waste material. Nowadays, waste materials or pozzolans from industrial and agricultural by-products such as fly ash and rice husk ash are receiving more attention since their uses generally improve the properties of the blended cement concrete, the cost, and the reduction of negative environmental effects (Rukzon and Chindaprasirt, 2008; Chindaprasirt et al., 2008).

Moreover, it is a well known fact in the field of construction materials that potential of some secondary raw materials can be significantly increased and used after their adjustment. The result is higher extent of valorization even of wastes that were not suitable in their original form. At the same time, parameters are improved, or new parameters appear.

Fly ashes in finegrain form can be used in concretes as:

- additive

- component of inorganic materials for secondary protection of the concrete.

By applying both classic and unusual adjustment methods it is possible to modify parameters of fly ashes to improve them for a particular purpose of use. Adjustment of fineness of the particles is one of the ways to improve usability of wastes and possible improvement of building materials parameters (Želinková et al., 2013; Želinková, 2014).

One of the ways how to use fly ash is preparing geopolymer mixtures. Geopolymers fall into a class of aluminosilicate binding materials synthetized by alkali activation of solid aluminosilicate raw materials such as fly ash, GGBS (ground granulated blast furnace slag) etc., with an alkali metal hydroxide and silicate solution. The utilization of fly ash in the development of geopolymeric materials for construction purposes has been and still continues to be a subject of many research studies (Balaguru et al., 2004; Davidovits, 2008; Ravindra and Ghosh, 2009; Temuujin et al., 2010).

The effect of the fineness of fly ash on geopolymer materials properties is also widely discussed. Changes induced in material during the mechanical activation process include reduction in particle size, changes in particle morphology, increase in specific surface area, structural defects formation, decrease in crystallinity degree, implying structural rearrangement. The most important consequence of transformation that occurs in material during the mechanical activation is its enhanced reactivity. Mechanical activation, as a method which can improve FA reactivity, is often applied for different applications of this material. Improved reactivity is primarily the result of increased particle fineness and formation of amorphous regins in structure. Finer particles of FA represent more reactive material without extra mechanical treatment. It is known that particles below 45 µm, obtained through various methods of separation, tend to improvement of mechanical strength of mortar when used as a supplementary cementitious material (Marjanović et al., 2014). Although there are numerous data relating to the mechanical activation of FA, the literature concerning the application of mechanically activated FA for the geopolymer synthesis is rather scarce. The main advantage of using mechanically activated FA in synthesis of geopolymers is the possibility of total utilization of FA, and not only its specific (finer) fraction.

This paper is engaged to possibilities of preparing the geopolymer mixtures based on modified (ground) fly ash, which was used in specific percentage combinations with unground (original) fly ash. As a modification, sludge from process of washing the crushed aggregates was used into the next mixture as filler. Finally, standard cement mixture using the same filler was prepared for testing. The results were analysed in the terms of possible application to protect of surface of concrete by coating.

- Materials and Methods

The materials for tested mixtures were as follows:

- Original fly ash - PVT (from Heating plant Kosice). The calcium oxide content of fly ash is less than 10%; hence it can be classified as Class F according to ASTM 618 standard,

- Ground fly ash - T60S1:  the same fly ash (time of grinding: 60 minutes, grinding ratio – mass of ground material to mass of grinding balls: 1/17),

- Ground granulated blast furnace slag (GGBFS):  as geopolymer intensificator,

- Na2SiO3+ NaOH as geopolymer activator,

- Sludge, the material from process of washing the crushed aggregates, coming from the sludge bed of the IS - Lom s. r. o, Maglovec,

- Ordinary Portland Cement (CEM I 42.5 R, Holcim, Turna nad Bodvou).

The granulometric and chemical composition of fly ashes, GGBFS, cement, sludge (fraction under 125 μm sieved from unground sludge) are given in Tab. 1, also in Tab. 2 (granulometric composition of unground sludge by sieving). The granulometric composition is expressed by following parameters – grain size: d (0.1) – indicates that 10% of the whole amount of investigated sample is under measured value of the particle size and the similar parameters d (0.5) – 50%, d (0.9) – 90% and the parameter dm - mean particle diameter.

Table 1. Chemical composition and results of granulometric analysis of input materials

|  | Oxide Composition [%] |  |  |  |  |  |  | Grain size [μm] |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Materials | SiO2 | CaO | MgO | Fe2O3 | Al2O3 | TiO2 | K2O | d(0.1) | d(0.5) | d(0.9) | dm |
| PVT (unground) | 51.11 | 2.58 | 1.18 | 6.40 | 23.21 | 0.96 | 1.81 | 3.97 | 20.44 | 84.73 | 74.10 |
| T60S1 (ground) | 49.72 | 2.49 | 1.09 | 6.37 | 22.32 | 0.94 | 1.73 | 3.48 | 14.53 | 52.81 | 31.02 |
| GGBFS | 41.28 | 35.98 | 12.85 | 0.39 | 6.30 | 0.60 | 0.54 | 3.61 | 19.03 | 111.5 | 49.46 |
| Cement | 19.87 | 64.36 | 4.61 | 3.18 | 3.99 | 0.21 | 0.30 | 3.20 | 17.69 | 49.57 | 29.90 |
| Sludge under 125 μm | 42.66 | 5.83 | 5.04 | 6.54 | 11.19 | 1.72 | 0.98 | 17.49 | 82.50 | 149.8 | 83.55 |

Table 2. Granulometric composition of sludge

| Fraction [mm] | Mass yield [wt. %] |
| --- | --- |
| 2 - 1 | 20 |
| 1 - 0.5 | 14 |
| 0.5 - 0.25 | 21 |
| 0.25 - 0.125 | 21 |
| <0.125 | 24 |

Design of mixtures composition was designed on the base of various literary sources (Yazici et al., 2012; Rangan, 2008; Škvara et al., 2005; Palomo et al., 1999; Palomo et al., 2011). The basic geopolymer mixture was intended in the terms of alkali-activated fly ash as microfiller. Alkaline activating agent for mixtures T1 – T4 was prepared by mixing the Na2SiO3, NaOH and GGBFS. The SiO2 to Na2O ratio (Ms Modul) in the alkaline activating agent was adjusted by 8 M NaOH addition to Na2SiO3 with a modul Ms = 2.5. Design of the combination Na2SiO3 and NaOH for preparing activator and its ratio to the other components in mixtures is given in Tab. 3, as well as recommendations summarized from various research reports (Yazici et al., 2012; Rangan, 2008; Škvara et al., 2005; Palomo et al., 1999; Palomo et al., 2011).

Table 3. Conditions of geopolymers preparing

| Parameters |  | Relationship between the geopolymer components |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Recommendations according to literature | Investigated mixtures |  |  |  |  |
|  |  |  | T1 | T2 | T3 | T4 | T5 |
| 1 | Water from the alkaline activators /geopolymer solids ; l/s | 0.19 | 0.19 | 0.19 | 0.19 | 0.25 | / |
| 2 | Alkaline solution/fly ash | 0.25-0.45 | 0.38 | 0.38 | 0.38 | 0.56 | / |
| 3 | Na2SiO3/NaOH | 1-1.25 | 1.18 | 1.18 | 1.18 | 1.18 | / |
| 4 | water/solids | 0.23-0.51 | 0.24 | 0.26 | 0.30 | 0.33 | 0.37 |

The representation of individual components and percentage of constituents in tested mixtures T1 – T5 are characterized in Table 4.

Table 4. The composition of experimental geopolymer mixtures

| Composition of fillers |  | Mixtures |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| [%] |  | T1 | T2 | T3 | T4 | T5 |
| Ground fly ash |  | 100 | 50 | - | 70 | 70 |
| Unground fly ash | 46% of mixture volume | - | 50 | 100 | - | - |
| Sludge |  | - | - | - | 30 | 30 |
| Presence of other components |  |  |  |  |  |  |
| GGBFS | 20% of fly ash | • | • | • | • | - |
| Na2SiO3 | 16% of fly ash | • | • | • | • | - |
| 8M NaOH | 16.5 % of fly ash | • | • | • | • | - |
| Cement |  | - | - | - | - | • |
| Water |  | • | • | • | • | • |
| Plasticizer |  | • | • | • | • | • |

The samples with the dimensions of 4x4x16 cm were kept at the laboratory temperature in the environment with the relative humidity of 50% for 28 days; dry bulk density, compressive and flexural strength, absorptivity and capillarity, were then determined. In accordance with standards, the methods of testing of mixtures were as follows:

- Dry bulk density (STN EN 1015-10, 2001)

- Compressive and flexural strength (STN EN 1015-11, 2001)

Sorption properties were tested in view of the intended function of tested materials: protective coating of concrete structures.

- Absorptivity and capillarity (STN 73 1316, 1989)

Absorptivity

After drying to constant mass, whole body of sample is immersed in water. After saturation of sample to constant mass was the specimen weighted. Absorptivity was calculated by use of the formula (2):

(2)

where:

ms – weight of saturated sample (g)

md – weight of dry sample (g)

Capillarity

After drying to constant mass, one face of the specimen is immersed in 5 to 10 mm of water a specific period of time and the increase in mass was determined. Standard periods are 10 min. and 90 min., for this experiment were determined and measured following intervals: 5, 15, 25, 35, 45, 55, 65, 75, 85, 90 minutes. Capillarity was calculated by use of the formula (1):

(1)

where:

ms– weight of saturated sample (g)

md – weight of dry sample (g)

For comparison, as additional method, capillarity as a result of height to which water soak (in cm) was tested during the previous test. The results were determined as the arithmetic mean of measurements on 4 sides of the samples.

- Results and discussion

The results of bulk density, water absorptivity and strengths are indicated in Table 5. The values of density are in the range of 1480 - 1760 kg/m3. The values of water absorption are in the range of 15.17- 20.93 %. Sample with highest value of density (T4) has the lowest value of water absorptivity. The trend of increasing water absorptivity with decrease of density is in accordance with known literature data. Values of compressive and flexural strength of investigated samples were in range 15.75 – 5.44 MPa (Rc); 1.62 – 3.93 MPa (Rf).  Results of compressive strength and principally also results of flexural strength confirm the known tendency as well – values increase with increasing density.

Table 5. Density, water absorptivity, capillarity, compressive Rc and flexural strength Rf        (28 days)

| Sample | Bulk density [kg/m3] | Water absorptivity [%] | Capillarity [%] after 90 minutes | Strength |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | Rf [MPa] | Rc [MPa] |
| T1 | 1744 | 15.25 | 4.45 | 2.19 | 11.64 |
| T2 | 1515 | 18.11 | 5.25 | 1.62 | 5.72 |
| T3 | 1477 | 20.93 | 6.45 | 2.45 | 5.44 |
| T4 | 1761 | 15.17 | 4.08 | 3.93 | 15.75 |
| T5 | 1639 | 19.75 | 4.30 | 2.71 | 11.36 |

In assessing properties of the samples T1 – T4, the following findings are resulting:

- Values of compressive strength and density of the samples based on fly ash are increasing from sample T3 after sample T1 (in terms of using share of ground samples of fly ash in mixture), while water absorption and capillarity decreases.

- The sample T4 (substituting 30% of ground fly ash by sludge) comparing to sample T1, shows in fact the similar value of bulk density, as well as values of the water absorption and capillarity. Sludge in the mixture T4 caused a slight increase in compressive strength of about 3 MPa; the sludge had positive effect on increasing of compressive strength value.

In assessing the samples T1 - T4 with a reference sample T5, the following findings are resulting:

- In terms of strength: sample T1 achieved approximately the same strength value (11-12 MPa). The presence of sludge in the recipe T4 caused an increase of compressive strength about 25%. T1 and T2 were reached only the half value of compressive strength compared to T5.

- In terms of absorptivity: the value of water absorptivity of the sample T4 was the lowest of all investigated samples (15%).  The reference sample T5 had approximately the same value of absorptivity as sample T3 (20%).

- In terms of capillarity: capillarity of T5 is approximately on the same level as T1 (4.3%).

Results of capillarity expressed by height of saturation are given in Figure 1.

Figure 1. Results of capillarity expressed by height of saturation in cm (28 days)

As can be seen in Figure 1, the lines of values of capillarity are divided into three sections. The first section contains the value of capillarity for the samples T1 and T3, in the middle part it is T2 and in the last part was resulting values for T4 and T5. It is caused by used components in recipe with various percentage ratios. Specimens T1 and T3 had similar composition – the main component was fly ash (100% fly ash in mixture). T4 and T5 had the main components sludge and fly ash. Sample T2 had similar trend as a curves for T1 and T3 but in lower values. T2 had the main component fly ash (ground and unground; 50/50 %).

The capillary action (in cm) on the surface of investigated samples was high by T1 and T3 (Fig. 1), but in assessing according the percentage of the weight of capillarity after 90 minutes were observed the maximum value by the sample T2 and T3 (samples which containing original fly ash in mixture).

The samples T4 and T5 had slowly and steady progress of absorption, according to Figure1. In terms of capillarity (in percent by weight, Tab. 5) T1, T4 and T5 had lower value (4%) of capillarity than T2, T3 (5-6%).

- Conclusion

The results indicate the effect of ground fly ash for production of geopolymer mixtures. The properties of geopolymers were measured at 28 days after hardening. The durability properties such as water absorption and capillarity showed a decreasing trend with the increase of fly ash fineness. Hence, it is concluded that increasing the fineness of fly ash increases its reactivity, and, hence, grinding is an effective way to enhance the performance of fly ash. When the volume of ground fly ash is increasing, it will fill the voids, increasing the density and hence preventing water absorption. The samples with a higher density by utilization of ground fly ash for geopolymer mixtures caused increases of resulting compressive and flexural strength.

The treatment of raw materials may enhance some of geopolymers parameters, while deteriorating others. Not only are the final parameters of geopolymer, but also the technological, e.g. consistency, compatibility, setting time etc. affected. Therefore any way of treatment and optimization of entry raw materials is a result of looking for limiting values and interactions, followed by establishing priorities and applying compromises.

Practical implications

The obtained results of slected properties of geopolymers with different portions of ground fly-ash show that the portion of the original and ground fly ash influences the final properties of geopolymer. The best results were identified in the recipe of T4 (70% of ground fly ash, 30% sludge). Fly ashes and other mechanically modified of secondary raw materials (slag, sludge, waste glass, ceramic waste etc. ...) improve the possibilities of using of secondary raw materials and for reuse in new building materials. In the aim of the research is orientation on the use of mechanically modified fly ash used as a microfiller in mixtures, to serve as a protective coating (plaster).

Acknowledgements

The author is grateful to the Slovak Grant Agency for financial support of the project VEGA 1/0767/13.

References

Balaguru, P. N., Nazier, M., Arafa, M. 2004. Field implementation of geopolymer coatings. Final report. Rutgers - The State University, 2004. [online] Published 19.10.2011. [citied 09.02.2012]. Accessible from <https://cait.rutgers.edu/files/FHWA-NJ-2002-011.pdf>.

Davidovits, J. 2008 Geopolymer Chemistry and Application. France: Saint Quentin, Institut Géopolymére, 2008. ISBN 978-29-514-8201-2.

Chindaprasirt, P., Rukzon, S., Sirivivatnanom, V. 2008. Resistance to chloride penetration of blended Portland cement mortar containing oil fuel ash, rice husk ash and fly ash. Construction of Building Materials [online] May, 2008. Volume 22, Issue 5, pp. 932-938. [citied 10.05.2012]. Accessible from <http://www.sciencedirect.com/science/article/pii/S0950061806003503>.

Marjanović, N., Komljenović, M., Baščarević, Z., Nikolić, V. 2014. Improving reactivity of fly ash and properties of ensuing geopolymers through mechanical activation. Construction and Building Materials [online] 25.02.2014 . Volume 57, pp.151-162. [citied 10.05.2015]. Accessible from <http://www.sciencedirect.com/science/article/pii/S0950061814001305>.

Michalíková, F., Floreková, L., Benková, M. 2003. The characteristics of energy waste – fly ash. Utilization of technologies for the environmental management. Kosice, 2003, pp. 228, [citied 12.10.2009] ISBN 80-8073-054-7.

Palomo, A., Grutzeck, M. W., Blanco, M. T. 1999. Alkali-activated fly ashes. A cement for the future. Cement and Concrete Research. [online] 21.09.1999. Volume 29. 1999. pp. 1323-1329. [citied 12.10.2009]. Accessible from <http://www.sciencedirect.com/science/article/pii/S0008884698002439>.

Palomo, A., Fernández-Jiménez, A. 2011. Alkaline activation, procedure for transforming fly ash into new materials. World of Coal Ash (WOCA) Conference. USA. 2011. [online] 15.03.2011. [citied 05.05.2011]. Accessible from <http://www.flyash.info/2011/205-palomo-2011.pdf>.

Rai, A., Rao, D.B.N. 2005. Utilisation potentials of industrial/mining rejects and tailings as building materiále. Management of Environmental Quality: An International Journal, Volume 16. Issue 6, pp.605 – 614.

Rangan, B. V. 2008. Fly ash-based geopolymer concrete. Curtin University of Technology. Engineering Faculty. Research Report GC 4. Perth, Australia. 2008. [online] September, 2009. [citied 02.02.2010].

Ravindra N. T., Ghosh, S. 2009. Effect of mix composition on compressive strength and microstructure of fly ash based geopolymer composites. ARPN Journal of Engineering and Applied Sciences. [online] Jun, 2009, Volume 4, Issue 4, 2009, pp. 68-73. [citied 02.02.2010]. Accessible from <http://arpnjournals.com/jeas/research_papers/rp_2009/jeas_0609_200.pdf>. ISSN 1819-6608.

Rukzon, S., Chindaprasirt, P. 2008. Development of classified fly ash as pozzolanic materials. Journal of Applied Science. [online] September, 2008. Volume 8, 2008, Issue 6, pp. 1097. [citied 08.04.2010]. Accessible from <http://www.researchgate.net/publication/46029158_Development_of_Classified_Fly_Ash_as_a_Pozzolanic_Material>.

STN 731316 (731316): 1989: Determination of moisture, water absorption and capillarity of concrete, national standard.

STN EN 1015-11: 2001: Methods of test for mortar for masonry. Part 11: Determination of flexural and compressive strength of hardened mortar.

STN EN 1015-10: 2001: Methods of test for mortar for masonry. Part 10: Determination of dry bulk density of hardened mortar.

Škvara, F., Jílek, T., Kopecký, L. 2005. Geopolymer materials based on fly ash. Ceramics – Silicate. [online] April, 2005. Volume 49, Issue 3. 2005. pp. 195-204. [citied 02.02.2009]. Accessible from <http://www.geopolymery.eu/aitom/upload/documents/ceramics_2005-03-195.pdf>.

TEMUUJIN, J. et al. 2010. Fly ash based geopolymer thin coatings on metal substrates and its thermal evaluation. Journal of Hazardous Materials. [online] April, 2010. Volume 180, Issue 1. 2010. pp. 748 - 752. [citied 16.05.2012].

Yazici, S., Arel, S. 2012. Effects of fly ash fineness on the mechanical properties of concrete. Sadhana. [online] Jun, 2012. Volume 37, Part 3. Indian Academy of Sciences. 2012, pp. 389-403. [citied 15.04.2015].

Želinková, M., Sičáková, A., Holub, M. 2013. Influence of Selected Grinding Specifications on the Fly Ash Granulometry. In: Procedia Engineering : Concrete and Concrete Structures 2013 : 6th International Conference, Slovakia. - Amsterdam : Elsevier. [online] Jun, 2013. Volume 65, pp. 39-44. Accessible from: <http://www.sciencedirect.com/science/article/pii/S1877705813015154>. ISSN 1877-7058.

Želinková, M. 2014. The analysis of particle size of fly ashes – the possibility of obtaining fine particles by grinding. In: Seminar PhD Students 2014: Environmental Engineering: proceedings. Volume 6. [CD-ROM]. Kosice : Technical University, 2014, pp. 72-80. ISBN 978-80-553-1914-8.